## 1.6. Surface Enhance Resonance Raman Scattering

## (SERRS)

1.6.1. Raman and Resonance Raman

The investigation of processes that occur when electromagnetic radiation interacts with molecules gives information about their structure. The phenomena widely studied are absorption, emission and scattering of the light. Each one is the basis of different spectroscopic techniques but the most important for this work is the scattering of light.  When radiation passes through a medium, the species present scatter a fraction of the beam in all directions. The Indian physicist Raman was the first to notice that a small fraction of the radiation scattered by certain molecules differs in wavelength from that of the incident beam and that the shift in wavelength can be linked to the structure of the molecule.75 His discovery was the beginning of the development of Raman spectroscopy.

Raman spectra are acquired by irradiating a sample with a powerful laser source.  It should be noted that classical and quantum theory show that there is one important requirement for the molecule to undergo Raman scattering and this is a change of polarizability of the molecule when irradiated.76

Three different types of scattered radiation are observed. When the incident radiation of energy h0 hits the sample, the collision with the photon excites the molecule from the ground electronic state to the virtual state of energy Ev. Immediately afterwards the photons are emitted and the molecule relaxes to the ground state. If the collision is elastic there is no exchange of energy between photon and molecule and no appreciable change in frequency. This scattering is called Rayleigh scattering and in that case the energy of scattering (Es) is equal to incident energy h0. If the collisions are inelastic there is an exchange of energy in two possible ways. The molecule can receive some energy from the photon (E) and get excited to a higher vibrational state. The scattered photon will then have a lower energy Es = h0 - E. This process is called Stokes scattering and the resulting shift in wavelength the Stokes shift. If, on the other hand, molecules give some energy to the photon, the resulting Es is equal to h0 + E and the wavelength is shifted to lower values as a result of anti-Stokes scattering.

Resonance Raman scattering is a phenomenon in which an intensity enhancement of the Raman scattering (normally about 103 to 104 for effective chromophore) occurs when the excitation source is used with a wavelength that closely approaches that of an electron absorption peak of the analysed molecule. One more advantage, apart of the intensity enhancement, of resonance Raman is that the excitation is mainly frequency specific for absorption bands and can yield electronic as well as vibrational information

Although Raman spectroscopy is suitable for the study of aqueous solutions and resonance Raman gives marked increases in intensity, the scattering is still sufficiently weak which makes it difficult to work with low concentration of samples. The discovery of the surface enhanced Raman effect in 1974 by Fleischmann et al. led to the development of a new area of analytical chemistry as well as raising the questions concerning the basic theory of surface enhanced Raman scattering and  the chemistry on the surface.77 Three years later, in 1977, surface enhanced resonance Raman scattering  (SERRS), which is a combination of resonance Raman and surface enhanced Raman scattering with enhancement of the Raman scattering claimed to be 1014-1015, was first observed by Van Duyne.78

The next section gives the overview of the basic theory behind SERRS as well as the applications. It should be noted that in many papers authors do not distinguish between SERS (which does not have a molecular resonance contributions) and SERRS. The theory behind both phenomena is based on the same principle, but the main differences lie in the size of enhancement and type of analytes used. Therefore, the development of SERRS theory and the application will be explained by referring to the published work on both types of Raman scattering.

1.6.2. Surface Enhanced Raman and Resonance Raman

Scattering

SERS is a phenomenon observed for a range of different molecules when they are adsorbed onto roughened noble metal surfaces. Although a generally accepted account of SERS is still not available, SERS has developed as an important analytical tool. The magnitude of the SERS enhancement is usually determined as an enhancement factor, which is the ratio between measured Raman cross section in the presence and in the absence of the metal surface. Typical values for enhancement range between 105 –106 for silver surface, although much larger enhancements of 1014 –1015 were recently reported in single molecule SERRS experiments using Ag and Au nanoparticles.79 The overall observed enhancement is generally explained in terms of  electromagnetic and chemical or  “first layer” enhancement.80

The electromagnetic enhancement theory of SERS describes enhancement as being caused by an amplification of the electric field due to the response of the material surface to the incoming light wave.81 The magnitude of the local field enhancement can vary depending on the material  (Au, Ag, Cu) and the coupling between different surfaces. Therefore, the mathematical model has to account for a number of important factors, especially the shape and the size of metal particles. Xu et al. used a theoretical model and experimental results of single molecule measurements to estimate the electromagnetic contribution to SERS.82 From their calculations it could be seen that in the case of nearly approaching Ag spheres, the enhancement factor is 1012 at 400 nm.  On average, enhancement factors of 1010 can be attributed to the electromagnetic enhancement.

Chemical enhancement results from the charge transfer excitation of chemisorbed molecules. In this mechanism is it assumed that an adsorbed molecule has donor or acceptor levels (highest occupied and lowest unoccupied molecular orbital) at the right energy so that the charge transfer complex with the surface metal at so called “active sites” might be formed.  Otto et al. reported that the strong electronic coupling between an adsorbed molecule and an active site generates new metal to ligand or ligand to metal charge transfer states that can be broadly excited at visible wavelengths.83  The percentage of the contribution of each factor to the overall enhancement is still the matter of continuous debate, although experiments showed that chemical enhancement contributes to the overall effect much less then electrochemical and accounts for the difference between the electromagnetic and the overall enhancement reported in literature (1013-1015).

Krug et al. investigated the influence of size and shape of nanoparticles on the surface enhancement.84 They screened Au particles of different sizes with adsorbed crystal violet molecules adsorbed on the surface and showed that SERS active particles have a narrow size range, about 63 ± 3 nm. Outside this range, particles have little or no SERS activity. They argue that in addition to the particle size, other factors like particle shape and specific adsorption sites are important for efficient optical enhancement. The faceted particle shape could be important because the sharp points and edges can act as “lightning rods” to concentrate the incident electromagnetic field. Sharp points could also function as active sites and are believed to be responsible for chemical enhancement via a resonant charge transfer process. Hilderbrand and Stockburger suggested that SERS active sites are high affinity binding sites associated with adsorbed anions such as Cl- and Br-.85 The number of active sites according to them is on average 3.3 per colloidal Ag particle.

The surfaces mainly used for SERS are silver and gold roughened surfaces. Using colloidal silver clusters, Kneipp et al.  detected  single adenine molecule using near infrared SERS showing that SERS could be used in detection of nucleotides in DNA sequencing.86 Recently, Xia and Sun published the results of their research of the synthesis of gold and silver nanoparticles which will prove to be very useful for the application in SER(R)S in the near future.87 They managed to make silver nanocubes with controllable dimensions (mean edge length of 175 nm) by a modified polyol process that involved the reduction of silver nitrate with ethylene glycol in the presence of a capping reagent such as poly(vinylpyrrolidone), PVP, at 160°C. The morphology and dimensions of the product were found to be strongly dependant on the reaction conditions. Subsequently, the authors also used silver nanocubes as templates to generate gold nanoboxes with a well defined shape. Since the optical and electrical properties as well as SERS enhancement, depend on the size and shape of the metal particles, it is clear that the chemical synthesis of nanoparticles of controlled shape, size and structure will have a huge impact on the future applications of SER scattering.

The same roughened metal surfaces are used in SERRS detection. As mentioned before, SERRS requires molecular as well as plasmon resonance and the main disadvantage in using it as a detection technique arises from the need for a specific chromophore that matches the excitation frequency. A significant amount of work has been done in the synthesis of new dyes that have both the desired chromophore and the ability to bind to the metal surface.88

SERRS is especially useful in the detection of biologically important molecules and compounds present in low concentration. Constantino et al. used the enhanced sensitivity of SERR scattering to achieve single molecule detection.89 Bis(benzimidazo) perylene (AzoPTCD) was dispersed in the host fatty acid matrix using Langmuir Blodgett technique and transferred to the silver deposited films. The SERRS spectra were then taken and the area mapped proving that spectra came from the single molecule detected in the matrix.

Although both surface enhanced Raman and resonance Raman scattering are proving to be extremely useful in fundamental studies on the single molecule level, they are also important analytical tools. SER(R)S has been used to detect  a variety of different types of analytes present in low concentrations, including pollutants90, explosives91 and chemical warfare agents92. Recently, a glucose biosensor was developed using SERS detection on a silver film and the glucose level was quantitatively determined using partial least square method.93

Since Raman spectroscopy is suitable for studies of aqueous solutions, both SER and SERR scattering are used in the detection of important biological molecules, especially DNA. The interactions between anthracycline antibiotics, which have chromophore in the visible region, and DNA were investigated using SERRS.94 Vibrational information for the antibiotic molecules themselves and a drug-DNA complex enabled the understanding of the DNA-drug binding. It was also shown that different modifications of the drug molecule effect its interaction with DNA. In a similar study, Ermishov et al. investigated the effect of antibiotic netropsin on double stranded DNA by SERS, making a significant contribution to the understanding of conformational changes when small molecules bind to different sites.95

Other important processes involving DNA, such as hybridisation and bending were also investigated using advanced Raman technigues.96 The ability of DNA to wrap and bend around the substrates is important in packaging and transcription. Therefore, Gaerhart et al. prepared 14 nm protein sized gold particles and examined the adsorbtion and bending of 16 base pair DNA strands by SERS.97 They found that the intensity of the enhanced vibrational modes of the bases within the sequences is dependant on the intrinsic DNA curvature and the way DNA binds around nanoparticles. This enabled the fast identification of strait, kinked or bent DNA in the solution.

However, the use of SERRS in DNA detection is less straightforward. Biomolecules, like DNA, do not posses a chromophore in the visible region and a label must be incorporated into the molecule to allow detection. Moreover, they do not have the ability to attach to the metal surface. Therefore, the direct analysis of DNA by SERRS is not possible without labelling the molecule with SERRS active species.

Recent work in our group focused on the SERRS detection of modified DNA.98 Two fluorescent labels, HEX and rhodamine 6G were added to the 5’ terminus of DNA. A colloid was used as a SERRS active surface. HEX is negatively charged and does not adsorb on to the colloid surface, but it was placed next to the modified base that attached to the surface and therefore was forced to come to close proximity facilitating the surface enhancement. On the other hand, rhodamine 6G has amino groups that attached to the colloid easily. Modified oligonucleotides were detected at about 2x10-13 mol dm-3. Moreover, it was possible to discriminate between labels in a mixture without the separation. However, the problems with the surface attachment decreased the reproducibility of the measurements. Therefore a new approach made use of benzotriazole monoazo dyes specifically designed to attach strongly to the surface and provide reliable SERRS spectra.

Benzotriazole dye phosphoramidite was synthesised and coupled to a DNA sequence during automated synthesis.99 In this way DNA was labelled at the 5’ terminus with the dye that was acting both as chromophore and surface attaching group. Although good SERRS spectra were obtained, synthesis of dye phosphoramidites is tedious.  Therefore, there was a need for a new, simpler and more effective approach.

Taking into account all these requirements and the work done previously on benzotriazole (BT) maleimides as a bifunctional reactant for SERS100, Diels Alder cycloaddition was chosen as most suitable reaction to be investigated. Diels Alder cycloaddition describes the reaction between two groups of molecules referred to as the dienophile (e.g. vinyl groups, maleimide) and the dienes (e.g. furan).

Aqueos conditons

diene

cycloadduct

# Dienophile

+

Not SERRS active (oligo, peptides)

SERRS active (benzotriazole dye)

SERRS active oligo

Scheme 1.1.  Attachment of the non SERRS active molecules to the surface using

Diels Alder cycloaddition.

+

SERRS active oligo

If a BT dye with a maleimide functional group is synthesised, it would produce a cycloadduct with diene modified DNA therefore enabling fast, reliable, simple labelling of oligonucleotides in an aqueous environment.

This concept was investigated together with the use of SERRS as a novel technique in detection of single and dual labelled olligonucleotides and the results are presented in this thesis. In Chapter 2 the synthesis of SERRS active benzotriazole dyes is discussed. Chapter 3 presents the study of SERRS surfaces used throughout the project.  The SERRS properties of dyes are discussed in Chapter 4. Labelling and SERRS detection of oligonucleotides is described in Chapter 5 with the special section on labelling of DNA with fluorescent molecules using novel labelling chemistry. Finally, Chapter 6 is based on the study of the fluorescence quenching properties of benzotriazole dyes and the design and function of a novel type of bioprobe, SERRS Beacons. Main conclusions are given in the Chapter 7 and all experimental procedures are described in detail in Chapter 8.

+