8.1. Synthesis and properties of benzotriazole dyes and

dye maleimides

8.1.1. General

All chemicals were purchased from Aldrich Ltd. except for 5- aminobenzotriazole (Lancaster Synthesis Ltd), cobalt naphthenate (Fluka). 1H NMR spectra were recorded on a Brücker 400 (400 MHz) instrument. Mass spectra were recorded on a JEOL AX505 spectrometer using chemical ionization (CI) or Fast Atom Bombardment (FAB) in a 3-nitrobenzyl alcohol matrix. Flash chromatography was carried out using silica gel 60 (Merck) or Biotage prepacked silica columns when automatic Biotage flash chromatography apparatus was used. Thin layer chromatography was carried out on aluminium sheets, coated with silica gel 60 F254, 0.2 mm layer (Merck) (A) EtOAc-hexane (1:1); (B) DCM-MEOH (9:1); (C) EtOAc-hexane 1:1.5. UV/Vis absorption spectra were measured using a Cary Bio300 UV-Vis spectrometer using quartz glass cuvettes with path length 10 mm. Melting points were measured using a Buchi melting point B-545 apparatus and are uncorrected.

8.1.2. Synthesis of benzotriazole dyes

4- (4’-Methoxy-phenylazo)-3H-benzotriazole-5-yl amine [1]

p-Anisidine (2.50 g, 20.0 mmol) was dissolved in HCl (50:50, 6 ml) and diazotised by dropwise addition of sodium nitrite (1.67 g, 24.0 mmol, in 15 ml H2O) at 0oC. An excess of nitrous acid was detected using starch-potassium iodide paper. 5-Aminobenzotriazole (2.44 g, 0.018 mol) was dissolved in sodium acetate buffer (pH 6, 80 ml) and methanol and the diazonium solution added dropwise to the coupling agent at room temperature to form a brown precipitate. After filtration the residue was washed with distilled water and then dried to yield the title compound as a brown powder (4.54 g , 85 %): Rf (A) 0.41; mp 218.0 C; 1H NMR  δH(acetone-d6): 3.87 (3H, s, CH3); 6.60 (2H, br s, NH2), 6.94 ( 2H, d, J8.9, H-4), 7.05 ( 2H, d, J8.3, Ar-H), 7.82 (1H, d, J8.9, H-5), 8.15 (2H, d, J8.5, Ar-H), 14.51 (1H, br s, NH); max (MeOH-H2O)/nm: 443.2 (/dm3 mol-l cm-116036); m/z (CI) 269.11562 [C13N6OH13 (M+H)+  2 ppm]; Anal. Calc. for C13H12N6O: C, 58.20; H, 4.51; N, 31.33. Found: C, 57.71; H, 4.07; N, 30.81.

4- (3’-Methoxy-phenylazo)-3H-benzotriazole-5-yl amine  [2]

Following the same procedure as for the synthesis of 1, m-anisidine (1.50 g, 12 mmol) and 5-aminobenzotriazole (1.60g, 10 mmol) afforded the title compound as a brownish-orange powder (2.62 g, 81%); Rf (A) 0.39; mp 205.6 C; 1H NMR δH(acetone-d6): 3.83 (3H, s, CH3), 6.80 (2H, br s, NH2), 7.02 (2H, m, Ar-H), 7.42 (1H, d, J8.3, H-4), 7.75 (2H, m, Ar-H), 7.83 (1H, d, J8.5, H-5), 14.47 (1H, br s, NH); max (MeOH-H2O)/nm: 438.0 (/dm3 mol-l cm-1 12036); m/z (CI) 269.11589 [C13N6OH13 (M+H)+ 3 ppm] ; Anal. Calcd. for C13H12N6O: C, 58.20; H,4.51; N, 31.33. Found: C, 58.58; H, 4.45; N, 28.83.

4- (3’,5’-Dimethoxy-phenylazo)-3H-benzotriazole-5-yl amine [3]

Following the same procedure as for the synthesis of 1, 3,5 -dimethoxyaniline (0.50 g, 4.0 mmol) and 5-aminobenzotriazole (0.40g, 3.0 mmol) afforded the title compound as an orange powder (0.61 g, 62%): Rf (A) 0.45; mp 193-195 (decomp.); 1H NMR δH(acetone-d6): 3.84 (6H, s, 2xCH3), 6.57 (1H, m, Ar-H), 6.80 (2H, br s, NH2), 7.03 (1H, d, J8.9, H-4), 7.41 (2H, s, Ar-H), 7.84 (1H, d, J9.0, H-5), 14.53 (1H, br s, NH), max (MeOH-H2O)/nm: 439.0 (/dm3 mol-l cm-1 13667); m/z (CI) 298.11782 [C14H15N6O2 (M+H)+ 0.1ppm) Anal. Calcd. for  C14H14N6O2: C, 54.45 ; H, 4.93; N, 29.34. Found: C, 54.72; H, 5.08; N, 30,05.

4- (Naphthalen-1-ylazo)-3H-benzotriazole-5-yl amine  [4]

Following the same procedure as for the synthesis of 1, -aminonaphthalene (1.20 g, 8.0 mmol) and 5-aminobenzotriazole (1.02 g, 7.0 mmol) afforded the title compound as a red powder (0.96 g, 51%): Rf (A) 0.47; mp 194.0 C; 1H NMR δH(acetone-d6): 7.00 (2H, br s, NH2), 7.64 (4H, m, Ar-H), 7.85 (1H, m, Ar-H), 7.90 (1H, d, J8.9, H-4), 8.0 (2H, m, Ar-H), 8.86 (1H, d, J8.9, H-5), 14.57 (1H, br s, NH), max (MeOH-H2O)/nm: 462.0 (/dm3 mol-l cm-1 14314); m/z (CI) 289.11885 [C16H13N6 (M+H)+  3.0 ppm ; Anal. Calcd. for C16H12N6: C, 66.66; H, 4.20; N, 29.15. Found: C, 67.03; H, 4.32; N, 27.12.

7-(4’- Methoxy - phenylazo) –1H-benzotriazole-4-yl amine [5]

Following the same procedure as for the synthesis of 1, p-anisidine (0.70, 9.0 mol) and 4-aminobenzotriazole (0.84 g, 6.0 mol) afforded the title compound as an olive green powder (1.26 g, 75% yield): Rf (A) 0.34; mp 203.4 C; 1H NMR δH (acetone-d6):  3.82 (3H, s, CH3), 6.51 (2H, br s, NH2), 6.67 (1H, d, J8.2, H-5), 7.00 (2H, d, J9.0, Ar-H), 7.87 (1H, d, J8.2, H-6), 8.86 (2H, d, J9.0,Ar-H); max (MeOH-H2O)/nm: 425.0 (/dm3 mol-l cm-1 29813); m/z (CI) 269.11506 [C13H13N6O (M+H)+  0.1 ppm]; Anal. Calc. for C13H12N6O: C, 58.20; H, 4.51; N, 31.33. Found: C, 57.57; H, 4.98; N, 30.92.

8.1.3 Synthesis of the maleamic acids

3-[4-(4’-methoxy –phenylazo)-3H-benzotriazol-5-ylcarbamoyl] acrylic acid [6]

BT dye 1 (2.68 g, 10.0 mmol) was partially dissolved in DCM (40 ml) and maleic acid anhydride (1.92 g, 20.0 mmol in 10 ml DCM) was added portionwise over half hour. The reaction mixture was stirred at room temperature overnight to produce a brown precipitate, which was collected by filtration, washed with DCM and dried. (3.00 g, 82% yield): Rf (B) 0.10; mp 193C (decomp.); 1H NMR δH (DMSO-d6): 3.90 (3H, s, CH3), 6.43 (1H, d, J12, CHCHCO2H), 6.72 (1H, d, J12, CHCHCO2H), 7.17 (2H, d, J9.0, Ar-H), 8.23 (1H, d, J8.8, H-4),  8.33 (1H, d, J8.8, H-5), 8.43 (2H, d, J9.0, Ar-H), 10.93 (1H, br s, NHCO), 11.00 (1H, br s, CO2H), 15.74 (1H, br s, NH); m/z (FAB) 367.11534 [C17 H15N6O4 (M+H)+   0.4 ppm]; Anal. Calcd. for  C17H14N6O4: C, 55.74; H, 3.85; N, 22.94. Found: C, 54.96; H, 3.61; N, 22.21.

3-[4-(3’-Methoxy-phenylazo)-3H-benzotriazole-5-ylcarbamoyl) acrylic acid [7]

Following the same procedure as for the preparation of 6, BT dye 2 (1.00 g, 3.0 mmol in 40 ml DCM) and maleic acid anhydride (0.73 g, 7.0 mmol in 10 ml DCM) afforded 0.87 g of a light brown powder (yield 67%) identified as the title compound: Rf (B) 0.12; decomposes at 196C;  1H NMR δH (DMSO-d6): 3.93 (3H, s, CH3), 6.43 (1H, d, J12, CHCHCO2H), 6.373 (1H, d, J12, CHCHCO2H), 7.10 (1H, m, Ar-H), 7.51 (1H, m, Ar-H), 8.03 (2H, m, Ar-H), 8,25 ( 1H, d, J9.0, H-4), 7.92 (1H, d, J9.0, H-5), 10.55 (1H, br s, NHCO), 12.98 (1H, be s, -CO2H), 15.36 (1H, br s, NH); m/z (FAB) 367.11456 [C17H15N6O4 (M+H)+  2.5 ppm]; Anal. Calcd. for C17H14N6O4: C, 55.74; H, 3.85; N, 22.94. Found: C, 54.82; H, 3.99; N, 22.51.

### 3-[4-(3,5’-Dimethoxy-phenylazo)-3H-benzotriazole-5-ylcarbamoyl] acrylic acid [8]

Following the same procedure as for the preparation of 6, BT dye 3 (3.00 g, 10.0 mmol in 40 ml DCM) and maleic acid anhydride (2.00 g, 20.0 mmol in 10 ml DCM) afforded 3.15 g of a dark brown powder (yield 80%) identified as the title compound: Rf (B) 0.10; decomposes between 196-199C; 1H NMR δH(DMSO-d6): 3.91 (6H, s, 2xCH3), 6.43 (1H, d, J12, CHCHCO2H), 6.73 (1H, d, J12, CHCHCO2H), 6.77 (1H, s, Ar-H), 7.70 (2H, s, Ar-H), 8.29 (1H, d, J9.0, H-4), 8.35 (1H, d, J9.0, H-5), 11.01 (1H, br s, NHCO), 13.05 (1H, br s, -CO2H), 15.76(1H, br s, NH); m/z (FAB) 397.12604 [C18H17N6O5 (M+H)+  2.6 ppm].

3-[4- (Naphtalen-1-ylazo)-3H-benzotriazole-5-ylcarbamoyl] acrylic acid amine [9]

The same procedure was followed as for the synthesis of 6. Dye 4 (0.25 g, 9.0 mmol) and maleic acid anhydride (0.17g, 2.0 mmol in 5 ml DCM) afforded the title compound as a dark orange powder (0.25 g, yield 75%): Rf (B) 0.12; mp 202C; 1H NMR δH (DMSO-d6): 6.43 (1H, d, J12, CHCHCO2H), 6.72 (1H, d, J12, CHCHCO2H), 7.00 (3H, m, Ar-H), 7.80 (2H, m, Ar-H), 8.16 (2H, m, Ar-H), 8.34 ( 1H, d, J8.2, H-4), 8.87 (1H, d, J8.1,H-5),  11.00 (1H, br s, NHCO), 12.97 (1H, br s, -CO2H), 15.82 (1H, br s, NH); m/z (FAB) 387.12109 [C20H15N6O3 (M+1)+  1.4 ppm]; Anal. Calcd. for  C20H14N6O3: C, 62.17; H, 3.65; N, 21.76. Found: C, 60.81; H, 3.41; N, 21.14.

.

8.1.4. Synthesis of the dye maleimides from maleamic acid

# 1-[4-(4’-Methoxy-phenylazo)-3H-benzotriazole-5-yl]-pyrrole–2,5-dione [10]

Method 1. A solution of dye 1 (0.50g, 2.0 mmol) in DMA (5 ml) was added dropwise to a stirred solution of maleic anhydride (0.18g, 2.0 mmol) in DMA (2ml). Then  cobalt naphthenate solution (0.02 ml cobalt naphthenate in 10 ml DMA) was added followed by acetic anhydride (0.40, 4.0 mmol) and the solution was warmed to 75ºC, stirred for 1 hour under nitrogen then cooled and diluted with water. The resulting precipitate was collected and washed thoroughly with water, then dissolved in DCM and filtered again to remove a dark brown insoluble precipitate. DCM was removed under reduced pressure and the brownish red solid purified by column chromatography using ethyl acetate/hexane (1:1.5) as an eluent. The resulting dark orange powder was identified as title compound (0.24g, 0.007 mol, 35% of yield): Rf (C) 0.57; 1H NMR δH (DMSO-d6): 3.90 (3H, s, CH3), 7.14 (2H, d, J9.0, Ar-H), 7.32 ( 2H, s, CH=CH), 7.58 ( 1H, d, J8.7, H-4), 8.10 (2H, d, J8.8, Ar-H), 8.39 (1H, d, J8.7, H-5), 16.05 (1H, br s, NH): max (MeOH-H2O)/nm: 386.0 (/dm3 mol-l cm-1 17353); m/z (CI) 349.10450 [C17H13N6O3 (M+H)+1.2 ppm]; Anal. Calc. for C17H12N6O3: C, 58.64; H, 3.47; N, 24.14. Found: C, 58.41; H, 3.68; N, 22.97.

The maleimide was crystallized from MeOH/H2O mixture giving orange needles. The melting point was not determined because the compound decomposes before it melts.

Method 2.To a solution of dye acid derivative 6 (0.30g, 1.0 mmol) in DMA (2 ml), cobalt naphthanete solution (0.01 ml in 10ml DMA) was added under nitrogen and heated to 40º C. Acetic acid anhydride (0.16 ml, 1.6 mmol) was then added and the reaction mixture warmed to 70-80ºC and stirred for 1 hour. A colour change from orange to deep red occured. The solution was cooled and diluted with water and the precipitate filtered off and redissolved in DCM. An insoluble solid was filtered off and the DCM removed under reduced pressure. A red powder was obtained using the Biotage flash chromatography system with ethyl acetate/hexane (1:1.5) to give a reddish orange powder identified as the title compound (0.14g, 51% yield).

Method 3. Dye acid derivative 6 (0.5 mmol) was dissolved in dichloromethane (20 ml)  and the resulting suspension cooled to 0ºC in ice water bath. To this cooled suspension was added in order of 1-hydroxybenzotriazole hydrate (0.07 g, 0.5 mmol)  and dicyclohexylcarbodiimide (0.31 g, 1.5 mmol). The reaction mixture turned green 5 minutes after the addition and was left to stir for 20 hours at room temperature. The precipitate which formed was filtered off and DCM removed under reduced pressure to leave a green powder which was purified twice by column chromatography using EtOAC/hexane (1.5:1) and DCM/MeOH (9:1) as eluents. Title compound was obtained as an orange powder (0.09 g, 53% yield).

# 1-[5-Amino-4-(4’-methoxy-phenylazo)-benzotriazole-1-yl] ethanone [11]

The above compound was isolated as a side product in preparation of 10 using method 1 after column chromatography purification using ethyl acatate/hexane (1:1.5) as an eluent. It is an orange solid with Rf (C) 0.50; 1H NMR δH(DMSO-d6): 1.91 (3H, s, -CH3), 3.89 (3H, s, -OCH3),  7.07 ( 1H, d, J8.8, Ar-H), 7.31 (1H, d, J9.0, H-4), 7.95 (2H, d, J8.8, Ar-H), 8.00 (1H, d, J9.0, H-5), 8.10 (2H, br s, NH2); Anal. Calc. for C15H14N6O2: C, 58.05; H, 4.52;. Found: C, 58.41; H, 4.78.  The compound was recrystallised from MeOH/H2O and orange crystals were obtained. The melting point was not determined as the compound decomposes prior to melting.

1-[4-(3’-Methoxy-phenylazo)-3H-benzotriazole-5-yl]-pyrrole-2,5-dione [12]

Following the same procedure as for the synthesis of 10 by Method 2, N-(2-azonaphthyl-3H-benzotriazole-6-yl) maleamic acid 7 (0.12 g, 3.0 mmol), cobalt naphthenate solution (0.01 ml) and acetic acid anhydride (0.06 ml, 6.0 mmol) afforded the title compound (0.11 g, 55% yield) as  a dark red powder after the purification by column chromatography using (DCM/MeOH (9:1 ): Rf (B) 0.68; 1H NMR δH (DMSO-d6): 3.89 (3H, s, -OCH3), 7.13 (1H, m, Ar-H ), 7.23 (2H, s, CH=CH),  7.49 (1H, t, J8.0, Ar-H), 7.62 (2H, m, Ar-H and H-4), 7.72 (1H, m, Ar-H), 8.39 (1H, d, J8.6, H-5), 15.26 (1H, br s, BT-NH); max (MeOH-H2O)/nm: 354.0 (/dm3 mol-l cm-1 11583);  m/z (FAB) 349.10454 [C17H13N6O3(M+H)+  1.1 ppm]; Anal. Calc. for C17H12N6O3: C, 58.64; H, 3.47; N, 24.14. Found: C, 58.24; H, 3.86; N, 23.24.

# 1-[5-Amino-4-(3’-methoxy-phenylazo)-benzotriazole-1-yl] ethanone [13]

# The above compound was isolated as a side product in the preparation of 12 using method 1 after column chromatography purification using DCM/methanol (9:1) as an eluent. It is an dark orange solid with Rf (C) 0.62; 1H NMR δH (DMSO-d6): 1.29 (3H, s, -CH3), 3.90 (3H, s, -OCH3), 7.14 ( 1H, d, J6.8, Ar-H), 7.30 (1H, s, Ar-H), 7.49 (1H, t, J8.0, Ar-H), 7.62 (1H, d, J8.6, H-4), 7.73 (1H, d, J6.8, Ar-H), 8.40 (1H, d, J8.6, H-5); max (MeOH-H2O)/nm: 342.0 (/dm3 mol-l cm-1 1015); Anal. Calc. for C15H14N6O2: C, 58.05; H, 4.52;. Found: C, 58.70; H, 4.31.  The compound was recrystallised from MeOH/H2O and orange crystals were obtained.

1-[4-(3,5’-Dimethoxy-phenylazo)-3H-benzotriazole-5-ylcarbamoyl]-pyrrole-2,5-dione  [14]

Following the same procedure as for the synthesis of 10 by Method 2, maleamic acid 8 (1.50 g, 3.8 mmol), cobalt naphthenate solution (10 l) and acetic acid anhydride (0.72 ml, 7.6 mmol) afforded the title compound (0.80 g, 56% yield) as an orange red powder after purification by column chromatography using (DCM/MeOH (9:1): Rf (B) 0.60; 1H NMR δH (DMSO-d6): 3.83 (6H, s, 2xOCH3), 6.74 (1H, s, Ar-H), 7.34 (2H, s, Ar-H), 7.40 (2H, s, HC=CH), 7.63 (1H, d, J8.4, H-4), 8.43 (1H, d, J8.5, H-5), 16.10 (1H, br s, BT-H); max (MeOH-H2O)/nm: 362.0 (/dm3 mol-l cm-1 13317);  m/z (FAB) 379.11548 [C18H15 N6O4(M+H)+  4.5 ppm]; Anal. Calc. for C18H14N6O4: C, 57.14; H, 3.73; N, 22.22. Found: C, 57.32; H, 4.00; N, 21.98.

1-[4- (Naphthalen-1-ylazo)-3H-benzotriazole-5-ylcarbamoyl]-pyrrole-2,5-dione [15]

Following the same procedure as for the synthesis of 10 by Method 2, N-(2-azonaphthyl-3H-benzotriazole-6-yl) maleamic acid 9 (0.12 g, 0.3 mmol), cobalt naphthenate solution (0.01 ml) and acetic acid anhydride (0.06 ml, 0.6 mmol) afforded the title compound (0.11 g, 55% yield) as  a dark red powder after the purification by column chromatography using (DCM/MeOH (9:1 ): Rf (B) 0.68; 1H NMR( δH(DMSO-d6): 7.37 (2H, s, CH=CH), 7.68 (3H, m, Ar-H),  7.81 (1H, m, Ar-H), 7.98 (1H, d, J8.2, Ar-H), 8.11 (1H, d, J8.2, Ar-H), 8.27 (1H, d, J8.0, Ar-H), 8.53 (1H, d, J8.7, H-4), 9.07 (1H, d, J8.7, H-5); max (MeOH-H2O)/nm: 400.2 (/dm3 mol-l cm-1 9389); m/z (FAB) 369.10217 [C20H13N6O2 (M+H)+  1.3 ppm]; Anal. Calc. for C20H12N6O2: C, 65.02; H, 3.30;. Found: C, 63.90; H, 3.42.

8.1.5. Synthesis of N-phenyl maleimides

3-(4-Amino-phenylcarbamoyl) acrylic acid [16]

1,4–Phenylenediamine (2.16 g, 20.0 mmol) was dissolved in DCM (20 mL) and maleic acid anhydride (1.96 g, 20.0 mmol) in DCM (5 mL) added dropwise over 30 min. After 12 h of stirring at rt, the resulting precipitate was collected, washed well with DCM and dried, giving the title product (3.93 g, 95%) as an orange powder, mp 179-181 C (decomp). Rf (A) 0.05. 1H NMR δH(DMSO-d6): 6.27 ( 1H, d, J 12.0, CHCHCO2H), 6.46 (1H, d, J 12.0, CHCHCO2H), 6.53 (2H, d, J 8.7, Ar-H), 7.31 (2H, d, J 8.7, Ar-H), 10.49 (1H, br s, -CO2H).  m/z(FAB) 207.07697 [C10H11N2O3 (M+H)+  1.5 ppm]. Anal. Calcd for C10H10N2O3: C, 58.25; H, 4.49; N, 13.60. Found: C, 58.28; H, 5.07; N, 13.13.

# N-[4-(2,5-Dioxo-2,5-dihydro-pyrrol-1-yl] acetamide [17]

Compound 16 (0.28 g, 1.4 mmol) was added to a solution of sodium acetate (0.11 g, 1.4 mmol) in acetic anhydride (5 mL). The reaction mixture was refluxed and after 5 min the acid dissolved and colour of the solution changed to pale yellow.  Stirring was continued for 1 h until TLC showed the reaction to be complete.  Water was added to the cooled solution and the pale yellow precipitate collected, washed with water and dried. The pure product was obtained after recrystallization from methanol as pale yellow powder (0.24 g, 85 %), mp 190-192 C (decomp). Rf (A) 0.48. 1H NMR δH(DMSO-d6): 2.80 ( 3H, s, CH3), 7.00 (2H, s, CH=CH), 7.27 (2H, d, J 8.8, Ar-H), 7.73 (2H, d, J 8.8, Ar-H), 9.25 (1H, s, NH).  m/z (FAB) 231.0769. [C12H11N2O3 (M+H)+  6.3 ppm]. Anal. Calcd for C12H10N2O3: C, 58.54; H, 4.10; N, 11.38. Found: C, 59.46; H, 4.51; N, 11.05.

5-[4-Amino-phenylimino]-5H-furan-2-one [18]

Method 1. 3-(4-Amino-phenylcarbamoyl) acrylic acid 16 (1.03 g, 5.0 mmol) was dissolved in DCM (20 mL) and cooled to 0°C. 1-Hydroxy benzotriazole (0.70 g, 5.0 mmol) and dicyclohexylcarbodiimide (1.24 g, 6.0 mmol) were added respectively. The colour of the solution changed to red after 2 h of stirring.  After 12 hours at rt, the precipitate was removed by filtration and the solvent removed under reduced pressure before the crude product was purified by column chromatrography eluting with MeOH in DCM(1:9) to give the title compound as an orange powder (0.60 g, 63%) .

Method 2. To a solution of acid derivative 16  (0.26 g, 1.26 mmol) in DMA (2 mL), cobalt naphthanate solution (0.01 ml, 0.06g in 10 mL DMA) was added under nitrogen and heated to 40º C. Acetic acid anhydride (0.12 mL, 2.52 mmol) was then added and the reaction mixture warmed to 70-80ºC and stirred for 2 h. The solution was cooled, diluted with water and the precipitate removed by filtration before dissolution in DCM.  The orange powder obtained after purification by flash chromatography with ethyl acetate/hexane (1:1.5) and recystallisation from ethyl acetate was identified as the title compound (0.17 g, 72 %), mp 185 C. Rf (B) 0.30. 1H NMR δH(acetone-d6): 5.10 (2H, br s, NH2), 6.65 (2H, d, J 8.8, Ar-H), 6.69 (1H, d, J 5.5, CH=CH), 7.35 (2H, d, J 8.8, Ar-H), 7.47 (1H, d, J 5.5, CH=CH).  m/z (FAB) 189.1262  [C10H9N2O2 (M+H)+  1.8 ppm]. Anal. Calcd for C10H8N2O2: C, 62.78; H, 4.68; N, 14.07. Found: C, 62.48; H, 5.89; N, 13.55.

# 3-(4-Nitro-phenylcarbamoyl) acrylic acid [19]

.

# Maleic acid anhydride (2.17 g, 22 mmol) was dissolved in THF (2 mL) and slowly added to a solution of 4-nitroaniline (1.53 g, 11 mmol) in THF (10 ml) and left to stir overnight at rt.  The yellow precipitate was collected, washed well with THF and dried giving the title compound as pale yellow powder (2.16 g, 83%), mp 193 C. Rf (A) 0.08; 1H NMR δH(DMSO-d6): 6.34 (1H, d, J 12.0, CHCHCO2H), 6.52 ( 1H, d, J 12.0, CHCHCO2H), 7.86 (2H, d, J 9.2, Ar-H), 8.24 (2H, d, J 9.0, Ar-H), 10.87 (1H, s, NHCO),  12.85 (1H, br s, CO2H). FAB-MS m/z  237.05123  [C10H9N2O5 (M)+  0.7 ppm]. Anal. Calcd for C10H8N2O5: C, 50.85; H, 3.41; N, 11.86. Found: C, 50.90; H, 3.40; N, 11.56.

# 1-(4-Nitro-phenyl)-pyrrole-2,5-dione [20]

# Following the same procedure as for the synthesis of maleimide 17, N-(4-nitrophenyl) maleamic acid 19 (2.16 g, 9.1 mmol) and sodium acetate (0.89 g, 10.9 mmol) were stirred in acetic acid anhydride (25 mL) at rt to give the title compound as a pale yellow powder (1.47 g,  74%) which was recrystallised from MeOH giving colorless plates, mp 162-164C; Rf (A) 0.38. 1H NMR δH(DMSO-d6): 7.26 ( 2H, s, CH=CH), 7.70 (2H, d, J 5.0, Ar-H), 8.36 (2H, d, J 5.1, Ar-H); CI-MS m/z  219.04058 [C10H7N2O4(M+H)+  2.5 ppm]. Anal. Calcd for C10H6N2O4: C, 55.10; H, 2.80; N, 12.84. Found: C, 54.80; H, 2.67; N, 12.63. Crystal structure deposited in Cambridge Crystal Database, accession number = 212029.

# 3-(3-Methoxy-phenylcarbamoyl) acrylic acid [21]

# Maleic acid anhydride (1.60 g, 16 mmol) was dissolved in THF (2 mL) and slowly added to the solution of 3-methoxy aniline (0.91 mL, 0.8 mmol) in THF (10 mL) and left to stir overnight at rt.  The  precipitate was collected, washed well with THF and dried giving the title compound as pale yellow powder (0.91g, 81%), mp 160 C. Rf (A) 0.1. 1H NMR δH(DMSO-d6): 3.73 (3H, OCH3), 6.31 (1H, d, J 12, CHCHCO2H), 6.45 ( 1H, d, J 12, CHCHCO2H), 6.66 (1H, d, J 8.2, Ar-H), 7.14 (1H, d, J 8.0, Ar-H), 7.22 (1H, t, J 8.0, Ar-H),  7.31 (1H, s, Ar-H), 10.35 (1H, s, NHCO),  13.05 (1H, br s, CO2H). m/z (FAB) 222.07663 [C11H12NO4(M+H)+  -4.2 ppm]. Anal. Calcd for C11H11NO4: C, 59.72; H, 5.01; N, 6.33. Found: C, 59.75; H, 5.11; N, 6.14.

5-[3-Methoxy-phenylimino]-5H-furan-2-one [22]

Following the same procedure as for the synthesis of maleimide 18, N-(3-methoxyphenyl)maleamic acid (0.55 g, 2.5 mmol) and sodium acetate (0.25 g, 3.0 mmol) were stirred for 30 min in acetic acid anhydride (10 mL) at rt and then extracted with DCM. The organic layer was dried over MgSO4 and evaporated to give the crude residue.  Column chromatrography with DCM-methanol (9:1) afforded the title compound as a yellow oil (0.42 g, 82 %). Rf(A) 0.45. 1H NMR δH(DMSO-d6): 3.73 (3H, s, OCH3), 6.83 (2H, d, J 8.3, Ar-H), 6.90 (1H, s, Ar-H), 7.11 (1H, d, J 5.6, CH=CH ), 7.28 (1H, m, Ar-H), ), 7.80 (1H, d, J 5.6, CH=CH). FAB-MS m/z 204.06605 [C11H9NO3(M)+  0.1 ppm]. Anal. Calcd  for C11H9NO3: C, 64.90 ; H, 4.43; N, 6.90. Found: C, 64.71 ; H, 4.82; N, 6.26.

# 3-(4-Methoxy-phenylcarbamoyl) acrylic acid [23]

# Maleic acid anhydride (2.17 g, 22 mmol) was dissolved in THF (2 mL) and slowly added to a solution of 4-nitroaniline (1.53 g, 11 mmol) in THF (10 ml) and left to stir overnight at rt.  The yellow precipitate was collected, washed well with THF and dried giving the title compound as pale yellow powder (2.16 g, 83%), mp 193 C. Rf (A) 0.08; 1H NMR δH(DMSO-d6): 6.34 (1H, d, J 12.0, CHCHCO2H), 6.52 ( 1H, d, J 12.0, CHCHCO2H), 7.86 (2H, d, J 9.2, Ar-H), 8.24 (2H, d, J 9.0, Ar-H), 10.87 (1H, s, NHCO),  12.85 (1H, br s, CO2H). m/z (FAB) 222.05815 [C11H12NO4 (M+H)+  -4.0 ppm]. Anal. Calcd for C11H11NO4: C, 59.72; H, 5.01; N, 6.33. Found: C, 59.47; H, 5.06; N, 6.09.

5-[3-Methoxy-phenylimino]-5H-furan-2-one [24]

Following the same procedure as for the synthesis of maleimide 18, N–(3-methoxyphenyl) maleamic acid (0.40 g, 1.8mmol) and sodium acetate (0.17 g, 2.0 mmol) were stirred 50 min in acetic acid anhydride (10 mL) at rt. The precipitate was collected, washed well with water and dried. Recrystallisation from acetone afforded the title compound as yellow needles (0.28g, 71 %).  Method 2 using Co naphthenate afforded the same product in 75% yield after purification with column chromatography using DCM-methanol (9:1) and recrystallization from acetone, mp 115 C (decomp). Rf (A) 0.50.  1H NMR δH(DMSO-d6): 3.77 (3H, s, OCH3), 6.98 (2H, d, J 7.0, Ar-H), 7.05 (1H, d, J 5.6, CH=CH ), 7.40 (2H, d, J 7.0, Ar-H), 7.75 (1H, d, J 5.6, CH=CH); EI-MS m/z (203.057 [C11H9NO3 (M)+  0.7 ppm].  Anal. Calcd for C11H9NO3: C, 64.90 ; H, 4.43; N, 6.90. Found: C, 64.44 ; H, 4.50 ; N, 6.53 .

3-(4-tert-Butoxycarbonylamino-phenylcarbamoyl) acrylic acid [25]

N-(4-Aminophenyl)maleamic acid 16 (0.43 g, 2.04 mmol) was dissolved in a mixture of dioxane, water and a 1M solution of sodium hydroxide (10 mL:5 mL:5 mL) at 0 C.  Di–ter-t butyl pyrocarbonate (0.48 g, 2.20 mmol) was added to the cooled solution and stirred for 45 min at rt.  The reaction mixture was concentrated under reduced pressure to 10 mL, cooled in an ice bath, covered with a layer of ethyl acetate (10 mL) and acidified with dilute aqueous potassium hydrogen sulphate (1M) to pH 2-3. The aqueous phase was then extracted with ethyl acetate (3 x 15 ml) and the combined organic phase washed with water (2 x 30 mL), dried over anhydrous sodium sulphate and evaporated in vacuo. The residue was dissolved in EtOAc, filtered and the filtrate triturated with hexane to give the title compound as a bright yellow powder (0.48 g, 85 %), mp 165 C. Rf (C) 0.05. 1H NMR δH (DMSO-d6): 1.40 (9H, s, 3 x CH3), 6.29 (1H, d, J 12.0, CHCHCO2H), 6.45 (1H, d, J 12.0, CHCHCO2H), 7.39 (2H, d, J 8.9, Ar-H), 7.50 (2H, d, J 8.9, Ar-H), 9.32 (1H, br s, NHCO), 10.40 (1H, br s, NHCO), 13.36 (1H, br s, CO2H), m/z (CI) (307.12950 [C18H17N2O5 (M+H)+ 2.8 ppm]. Anal. Calcd for C18H16N2O5: C, 58.80; H, 5.90; N, 9.15. Found: C, 58.65; H, 5.71; N, 8.96.

[4-(2,5-Dioxo-2,5-dihydro-pyrrol-1-yl)-phenyl] carbamic acid tert-butyl ester [26]

Compound 25 (0.25 g, 0.8 mmol) was added to DCM (50 mL) and the suspension cooled to 0ºC.  To the cooled stirred solution was added in order 1-hydroxybenzotriazole hydrate (0.13 g, 0.8 mmol) and morpho CDI (1.40 g, 3.3 mmol).  After 5 h of stirring, the reaction mixture was diluted with DCM (30 mL) and extracted successively with water (3 x 50 mL), 1M hydrochloric acid (1 x 40 mL) and sodium bicarbonate (1M, 1 x 40 mL).  The organic phase was dried (sodium sulphate) and the solvent removed. The title compound was obtained by recrystallization from methanol as pale yellow powder (0.19g, 83%), mp 179 C. Rf (C) 0.67. 1H NMR δH(DMSO-d6): 1.45 (9H, s, 3 x CH3), 7.14 (2H, s, CH=CH), 7.18 (2H, d, J 8.7, Ar-H), 7.52 (2H, d, J 8.7, Ar-H), 9.48 (1H, br s, NHCO). CI-MS m/z  289.11883 [C15H17N2O4 (M+H)+ 0.6 ppm]. Anal. Calcd for C15H16N2O4: C, 62.49; H, 5.59; N, 9.17. Found: C, 61.97; H, 5.42; N, 9.76.

8.1.6. Diels Alder cycloaddition

4-(Dimethyl-hydrazonomethyl)-2-phenyl – isoindole-1,3-dione [27]

Phenyl maleimide (0.10 g, 0.67 mmol) was dissolved in acetonitrile (2.5 ml) and added to the solution of 2-furaldehyde dimethylhydrazone (0.15 ml, 1.2 mmol) in an acetonitrile-water mixture (2.5 ml:5 ml). The reaction mixture was stirred at 40ºC for 15 minutes by which time TLC showed the reaction to be complete. After 2 days bright yellow needles were obtained from the solution and identified as the title compound (93% yield), mp 178.3 °C; Rf (A) 0.47; 1H NMR ( δH(acetone-d6): 3.80 (6H, s, 2xCH3), 7.44 (1H, s, HC=N), 7.50 (4H, m, Ar-H),  7.64 (1H, m, Ar-H), 8.29(1H, m, Ar-H), 8.15 (2H, m, Ar-H).

4-(Dimethyl-hydrazonomethyl)-2-[4-(4’-methoxy-phenylazo)-3H-benzotriazole-5-yl)-isoindole-1,3-dione [28]

Dye maleimide 10 (7 mg, 0.02 mmol) was dissolved in acetonitrile (2 ml) and water (6 ml). To this solution 2-furaldehyde dimethylhydrazone (0.005 ml, 0.04 mmol) was added and the reaction mixture stirred at 45C for 30 minutes by which time TLC showed the reaction to be complete. An orange precipitate was obtained from the solution on cooling and identified as the title compound (6 mg, 70% yield): Rf(C) 0.60; mp 185.0 C, 1H NMR δH(DMSO-d6): 3.12 (6H, s, 2xCH3), 3.83 (3H, s, CH3), 7.10 (2H, d, J8.9, Ar-H), 7.70 (2H, d, J8.9, Ar-H),  7.85 (1H, m, Ar-H), 8.00 (1H, s,  CH=N), 8.05 (2H, m, Ar-H), 8.16 (1H, d, J8.9, Ar-H), 8.38 (1H, d, J8.9,Ar-H), 15,62 (1H, br s, NH).

8.2. SERRS substrates

8.2.1. General

All chemicals were purchased from Aldrich Ltd. except for polyvinyl alcohol and aminomethylated polystyrene resin 100-200 mesh, which were obtained from Nova Biochem. Cover glass discs of 13 mm diameter and 21.5 mm thickness (BDH) were used in the preparation of PVA-Ag and cold deposited silver discs. Spin coater Electronic Micro Systems Model 4000-1 was used to prepare PVA-Ag substrates. Raman and SERRS spectra were recorded using a Renishaw 2000 Raman spectrometer with 514.5 and 785 nm excitation sources. Solid samples were used for obtaining Raman spectra and solutions of dye in methanol-water mixture were used for SERRS. Static spectra were obtained using 3 accumulations of 3 s and extended (200-2000 cm-1) using 2 accumulations in 10 s. Surface mapping of PVA –Ag discs coated with BT dye maleimide was performed using Renishaw Ramascope 2000 at 514.5 nm with xyz stage control using 5m steps for mapping  400x400m2 disc area. Electron probe microanalysis (EPMA) was done using Cameca SX100 instrument within the Department of Physics at the University of Strathclyde.

8.2.2  Silver colloid

The colloidal silver suspension was prepared by the method based on a report by Lee and Meisel.117 All glassware was soaked in aqua regia for at least 30 minutes prior to use and then rinsed well with water. 500 ml of distilled water was stirred vigorously and heated using a Bunsen burner. When the temperature reached 60ºC, silver nitrate (90 mg, 0.53 mmol) was added and the solution heated rapidly to about 95 –98ºC and trisodium citrate added (1.1 eq, 150 mg, 0.58 mmol). The temperature was maintained at 98ºC for a further 90 minutes, the heating stopped and the mixture stirred until the resulting greenish solution had cooled to room temperature. The quality of silver colloid was checked by UV/Vis spectroscopy. The colloid had a single narrow band at 402 nm and a full width at half maximum (FWHM) of approximately 51 nm (typical values are in the range of max = 400-404 nm and FWHW  60 nm).

8.2.3. Cold deposited Ag films

Silver vapor was deposited onto a glass surface. A small piece of thin silver wire was placed into the molybdenum substrate boat in an Edwards E306A vacuum evaporator. A high vacuum pump was used to evacuate the chamber to a final pressure of 1x10-5 mbar. The deposition rate and thickness were monitored using an Intellimetrics IL100 crystal thickness monitor. The glass pieces were held approximately 20 cm directly above and parallel to the substrate boat during the evaporation of the silver. Typical deposition rates of 0.01 –0.02nms-1 were used.

8.2.4. Polyvinyl alcohol (PVA) substrates

A slight modification of a procedure used by Vo Dinh was used to prepare polyvinyl alcohol - silver substrate deposited on glass discs. PVA (1.6 ml, 5% or 10 % solution in water) was stirred with silver nitrate (0.40 g) for 24 hours. A few drops of PVA - AgNO3 solution were distributed on the surface of the glass discs and the discs were then spun at 2350 rpm for 20 s to ensure uniform coverage of the glass. The coated discs were dried overnight at 60C under vacuum and then heated at 100C for two hours. Finally, the substrate was dipped in aqueous FeSO47H2O (wt/vol) for 30 s and then placed in an oven at 100C for 15 minutes.

8.2.5. TiO2 – silver discs

TiO2–silver discs were obtained from Professor A. Mills, Pure and Applied Chemistry, University of Strathclyde.

8.3. SERRS of dyes and dye maleimides

8.3.1. General

A Renishaw 2000 Raman spectrometer with 514.5 nm laser excitation was used for SERRS measurements.  The static spectra were recorded using 3 accumulations of 3 s and extended (200-2000 cm-1) using 1 accumulation in 10 s. The methanol-water solutions of dyes were use in SERRS measurements. Normal Raman scattering was obtained from a solid sample presented as fine powders on glass slides. UV/Vis absorption spectra were measured with a Cary Eclipse Varian UV/Vis spectrometer using quartz glass cuvettes with a path length of 10 mm. IR spectra of solid dyes were recorded with a Nicolet Avatar 360 FT-IR using the KBr method for sample preparation. Surface mapping of PVA –Ag discs coated with BT dye maleimides was performed using a Renishaw Ramascope 2000 at 514.5 nm with xyz stage control and applying 5m steps for mapping  400x400m2 disc area

8.3.2. Molecular modelling and frequency calculations

Density functional geometry optimizations and vibrational frequency predictions were calculated using the Gaussian98W program running on a Windows NT workstation. The BLYP method with the 6-31/G (d, p) basis set was used for all density functional calculations. The Raman frequencies predicted from calculations were used as an aid in assigning bands in both Raman and SERRS spectra.

8.4. Synthesis and labeling of modified oligonucleotides

8.4.1. General

The synthesis of the oligonucleotides was carried out using a Peseptive Biosystems Expedite 8909 system. All reagents were supplied by Applied Biosystems, except for the amino link which was purchased from Link Technologies. The estimated loadings of the columns were 1.0 μmol. The following sequences were used: probe 1: 5’- TCT CAA CTC GTA and probe 2: 5’- CGC ATT CAG GAT. Effective coupling of the amino link was ensured by double delivery to the column with an extended coupling time of 15 minutes. Butadiene phosphoramidite was made in our lab and  supplied by Dave Robson.

N – (2-Methoxy-penta-2,4-dienyl) succinamic acid [29]

Succinic anhydride (1.68 g, 17mmol) was dissolved in DCM (10 ml) and added dropwise to furfurylamine (1.00ml, 10 mmol). Reaction mixture was stirred for 3 h at rt. and the precipitate isolated by filtration, washed well with DCM and dried. The title compound was obtained as a white powder (2.10g, 95% yield): Rf (DCM-MEOH 9:1) 0.12; mp 122.9 C; 1H NMR δH(DMSO-d6): 2.34 (2H, t, J6.0, J7.6, COCH2), 2.44 (2H, t, J6.7,  J6.6, CH2CO2H), 2.23 (2H, d, J5.6, CH2NH), 6.21 (1H, s,  Fur-H), 6.98 (1H, s, Fur - H),  7.55 (1H, s, Fur - H), 8.31 (1H, s, NHCO), 12.05 (1H, br s, CO2H); m/z (EI) 197.06842 [C9H12NO4 (M+H)+   2.0 ppm]; Anal. Calcd. for  C9H11NO4: C, 54.82; H, 5.62; N, 7.10. Found: C, 54.25; H, 5.87; N, 7.09.

N-(4-[4-(4-Methoxy-phenylazo)-2,3-dihydro-1H-benzotriazole-5-yl)-3,5-dioxo-10-oxa-4-aza-tricyclo[5.2.1.0.2,6] dec-8-en-1-ylmethy) succinamic acid [30]

Dye maleimide 10 (0.20g, 0.57 mmol) was dissolved in acetonitrile (4 ml) and water (12 ml). To this, the solution of 29 (0.23g, 1.20mmol) was added and the reaction mixture stirred at 45C for 1.5 h by which time TLC showed the reaction to be completed. Product was extracted with 3x200mL of EtOAc and solvent removed in vaccuo. The solid was  redisolved in EtOAc and triturated with hexane to give  above compound as yellow solid (0.22g, 71%). Rf(C) 0.30; mp 111.2C; 1H NMR ( δH(DMSO-d6): 2.33 (4H, m, COCH2,CH2CO2H), 2.50 (2H, m, CH2NH), 3.88 (3H, s, 0CH3),  6.21 (1H, d, J5.0, CH=CH), 6.37 (1H,d, J5.0, CH=CH), 6.43 (1H, s, OCH), 7.21 (2H, d, J9.0, Ar-H), 7.51 (1H, d, J8.9, Ar-H), 7.55 (1H, s, COCH), 8.22 (1H, s, COCH), 8.27 (3H, m, 2xArH, CONH), 8.35 (1H, d, J8.9,Ar-H), 12.01 (1H, br s, COOH); 16.01 (1H, br s, BT NH). FAB-MS m/z  547.17372 [C26H24N7O7 (M+H)+ 0.4 ppm].

8.4.2. Synthesis of furan modified oligonucleotides [32a, b]

Compound 29 (0.024g, 0.12 mmol) was dissolved in anhydrous DMF (1 ml) and then activated by reaction with 1,1- carbonyldiimidazole (0.036g, 0.22 mmol). The mixture was warmed to 40˚C for 5 minutes and then allowed to come to room temperature. The resulting activated acid was loaded into a 1 ml syringe and attached to the column containing oligonucleotide probe 1. An empty 1 ml syringe was attached to the other end of the column, pushed through several times and then allowed to stand for 3 hours. After the time had elapsed, the solution was taken up into one syringe and removed from the column. The column was then washed well with DMF and acetonitrile and dried with nitrogen. The same procedure was repeated using the probe 2 sequence to obtain 33b.

8.4.3.  Synthesis of butadiene modified oligonucleotide [33]

Butadiene phosphoramidate  was allowed to couple onto the 5’end of probe 2 during automated synthesis. A 30 min coupling time was used.

8.4.4. Oligonucleotide deprotection and cleavage from solid

support

The oligonucleotide was deprotected and removed form the solid support using concentrated ammonia solution. Solid support with synthesised oligonucleotide was placed in an Eppendorf tube, 1 ml of concentrated ammonia added and heated at 55˚C overnight. Finally, the solution containing the deprotected oligonucleotide was placed in a  round bottom flask and the ammonia removed in vacuo. The solid oligonucleotide was redissolved in distilled water and purified by HPLC.

8.4.5. Synthesis of oligonucleotide cycloadducts

The furan-modified oligonucleotide 33a (500 μl of 8 x 10-6 mol dm-3) in phosphate buffer (25 mM, pH 5.5) was added to the benzotriazole dye maleimide (MeCN/H2O 3:7, 3eqs, 80 μl).  The volume was made up to 1 ml with phosphate buffer and MeCN to keep the amount of MeCN at 30%.  The solution was then heated at 40 0C for 150 mins to complete the cycloaddition.  50 μl aliquots were used for HPLC. The same procedure was followed in all cycloadditions performed.

8.4.6. HPLC purification of modified oligonucleotides

Purification of the oligonucleotides was carried out using a PE Biosystems Biocad Sprint HPLC system running Biocad software. For each sequence, an analytical run was carried out before a full preparative run was attempted. UV detection at 260 nm was used in each case. C-18 Chromolith column (flow rate 4 ml/s) and C-18 column (flow rate 1 ml/min) were used for purifications. The following reverse phase methods were developed (Buffer A = ammonium acetate pH 7, Buffer B = MeCN)

Method 1 for purification of furan modified oligos: 0-5 CV 5% B, 5-30 CV 5-30% B, 30-40 CV 30-100 % B, 40-43 CV 100% B. Total time for method to be completed 19.94 min.

Method 2 for purification of oligo cycloadduct:  0-5 CV 5% B, 5-15 CV 5-10% B, 15-35 CV 10-15% B, 35-45 CV 25-100% B, 45-48 CV 100% B. Total time for method to be completed 22.02 min.

Method 3 for purification of modified oligos using C-18 Supelco column: 0-5 CV 8% B, 5-10 CV 8-20% B,  10-21 CV 20-60% B, 21-23 CV 60-0% B. Total time for method to be completed 38.02 min.

8.4.7. Desalting procedure after purification

The pure oligonucleotide sample was dissolved in 1.0 ml of distilled water and passed through asize exclusion HiTrap Desalting column packed with G25 Sephadex Superfine matrix using PE Biosystems Biocad Sprint HPLC system running Biocad software. 15 minutes method was created and both conductivity and absorbance at 260 nm followed. The eluted product was collected in a round bottomed flask, the water removed in vacuo and the oligonucleotide redissolved in 1 ml water prior to storage.

8.4.8. Measurement of the concentration of the oligonucleotide

stock solutions

Using Beer Lambert Law the absorbance value at 260 nm of the stock solutions is converted into the concentration of oligonucleotide sample:

Beer Lambert Law:  A = abc   where   A = absorbance

a = absorption coefficient

b = path length (1 cm)

c = concentration

The absorption coefficient must be determined for each oligonucleotide is cumulative sum of the absorption coefficients of the individual DNA bases.:

#### A =  {(dG x n) + (dA x n) + (dC x n) + (dT x n)} x 0.9

where 0.9 represents a hypochromicity factor.

8.4.9. SERRS of the cycloaddition

When following the cycloaddition by SERRS a 1:1 ratio of furan-modified oligonucleotide to benzotriazole dye maleimide was used.  Copper (II) nitrate (100 μl, 0.01 M) solution was added to the reaction mixture to enhance the rate.

The reaction was followed by spotting 10 μl of the reaction mixture onto the PVA-silver coated surface. Spectra were taken using 514.5 nm excitation and 3 accumulations in 3 s.

8.4.10. Fluorescence measurements of labelled oligonucleotides

Cary Eclipse fluorimeter was used to measure the fluorescence of the labelled oligonucleotides. Disposable fluorescence cuvettes were used and all solutions of oligonucleotides were prepared in distilled water.

8.5. SERRS beacons

8.5.1. General

All fluorescence measurements were performed using a Cary Eclipse fluorimeter and disposable fluorescence cuvettes.  All solutions were prepared by dissolving used dyes and fluorophores in 70% water: 15% acetonitrile: 15% DMF. Cary Bio 300 UV/Vis spectrometer was used to obtain UV/Vis data.  Refractive indices of solvents to estimate the quantum yields were taken from the literature.

8.5.2. Design and purification of SERRS beacon

SERRS Beacon :	5’ BTDye – CGC ACC TCT GGT CTG AAA GTT TAT TGG 			TGC G - FAM

Exact Complement : 	5’ TTT TTT AAT AAA CTT TCA GAC CAG ATT TTT T

Mismatch : 		5’ TTT TTT AAT AAA CTT TTA GAC CAG ATT TTT T

Controls: 		5’ TTT GCG TAA GTC CTA AGA GTT GAG CAT TTT

(both provided by Dr. Enright)

5’ GCT GGA ACA GAG ACC ATA GCC GAC GT

The SERRS Beacons were produced by synthesising the desired sequence on a FAM CPG solid support (Transgenomic, Glasgow, UK) using an Expedite 8909 DNA synthesiser and adding the butadiene monomer as the final 5’-residue.  Cleavage and deprotection in concentrated ammonia at 50oC for overnight gave the 5’-butadiene 3’-FAM modified sequence, which was purified by reverse phase HPLC.  The benzotriazole azo dye maleimide (10 eq, phosphate buffer pH 5.5 with 30% MeCN) was added to the diene oligonucleotide and left for 12 hours at 40 oC in the dark.  The SERRS Beacon was purified by reverse phase HPLC on a C18 Supelco column with buffer A = 0.1 M triethylammonium acetate pH 6.5, buffer B = 0.1 M triethylammonium acetate with 75 % acetonitrile running from 20 to 70 % B over 25 minutes at 1 mlmin-1.  SERRS Beacon was then desalted using Sephadex column and dissolved in  1 ml of  hybridisation buffer (1 mM MgCl2, 20 mM Tris.HCl, pH 8.0).

8.5.3. Hybridisation Conditions

To the SERRS Beacon (50 l, 8.4x10-7 mol dm-3) in the hybridisation buffer wad added the desired sequence (5 equivalents) and solution made up to 100l with the buffer. The temperature was then increased to 80C and then slowly decreased to room temperature to enable hybridisation.

8.5.4.  SERRS measurements using silver colloid

Citrate reduced silver nanoparticles were produced as described in previous section.  For the analysis the SERRS Beacon mixture from above (25 l) was added to silver nanoparticles (260 l). When aggregating agent was used, 10 l of spermine tetrahydrochloride (1 x 10-5 mol dm-3) was added to 250 l of the colloid and 25 l of the SERRS Beacon solution. A final concentration of the SERRS Beacon was 3.7x 10-8 mol dm-3.  Extended SERRS spectra (200-2000 cm-1) were obtained with a  Renishaw Ramascope 200 with 514.5 nm excitation suing 5 accumulations in 10 sec. Different concentrations of silver colloid were used. To make up 50% silver colloid, 5 ml of stock colloid solution was diluted with 5 ml of distilled H2O. 25% colloid was made by diluting 2.5 ml of stock solution with 7.5 ml of distilled H2O.

8.5.5.  SERRS measurements using PVA-silver disc

The silver/PVA films were prepared as described previously.  The SERRS Beacon mixture (10 l) was added to the disc and left to sit for 20 minutes.  The film was washed well with water and then wet examined using the Renishaw Ramascope as before but using 10 % of the laser power.